Python Script: Conformational Entropy from MD Trajectory

Deng Hu, Hang Luo, Dou Zhang

The Cartesian coordinate-based conformational entropy was calculated from atomic trajectories obtained by molecular dynamics (MD) simulations. In polymers, changing monomer occupancy from a single component to random occupation diversifies the local chemical environment and introduces geometric and electronic mismatch. However, such sequence perturbation does not automatically lead to an entropy increase. Instead, the outcome depends on the structural characteristics of the modified unit, particularly its ability to regulate segmental torsional freedom, steric hindrance, and local charge–environment matching. Bridge units that more effectively disrupt regular packing and roughen the conformational energy landscape can expand the accessible conformational space and disperse collective fluctuations, thereby increasing conformational entropy.

Conformational entropy was used to quantify the number of accessible chain conformations and the breadth of their distribution. Under the same temperature and analysis protocol, a higher conformational entropy generally indicates a larger accessible conformational space and a higher degree of conformational disorder. Two entropy descriptors based on the covariance matrix of thermally induced atomic coordinate fluctuations were employed, namely the Schlitter upper-bound entropy, Schl, and the quasi-harmonic entropy, SQH. Both quantities were evaluated using the same trajectory preprocessing procedure and the same atom-selection criteria to ensure direct comparability among different polymers. The attached .txt file provides a Python-ready script for the calculation, while the trajectory files required for analysis should be exported separately from Materials Studio simulations.

(1) Trajectory Selection and Preprocessing

The equilibrated production trajectories, for which both the density and total energy had reached stable plateaus, were selected for statistical analysis. To eliminate the influence of overall translation and rotation on the covariance statistics, each frame was rigidly aligned to a reference structure using the Kabsch least-squares algorithm by minimizing the root-mean-square deviation (RMSD). The same atom-selection rule and chain-segment definition were adopted for all samples to ensure meaningful comparison. In this study, the full atomic set, including hydrogen atoms, was used for the entropy analysis.

(2) Mass-Weighted Covariance Matrix

For a selected set of N atoms, the Cartesian coordinates of frame t were reshaped into a 3N-dimensional vector, x(t) The mass-weighted coordinate vector was then defined as

y(t)=M1/2x(t)	(1)

where M is the 3N×3N diagonal mass matrix, in which the atomic mass of each atom is repeated along the x, y, and z components. All y(t) vectors were stacked into a matrix Y∈RF×3N, where Fis the number of frames. After mean-centering Y, the mass-weight covariance matrix was obtained as

Cm=⟨y-⟨y⟩y-⟨y⟩T⟩	(2)

To improve numerical efficiency and reduce memory consumption, the nonzero eigenvalues λiof Cm were obtained through singular value decomposition (SVD). Specifically, for the centered matrix Y, an economical decomposition,

Y=UΣVT	(3)

was performed, yielding

λi=σi2F-1	(4)

where σi denotes the singular values in 𝛴.

(3) Schlitter Conformational Entropy

The Schlitter entropy was calculated as an upper-bound estimate of conformational entropy according to

SSchl=kB2lndetI3NαCm      α=e2kBTℏ2	(5)

where kB is the Boltzmann constant, ℏ is the reduced Planck constant, and I3N is the 3N-dimensional identity matrix. In practice, the determinant term was evaluated in the eigenvalue form as

ln⁡det⁡I3NαCm=iln⁡1αλi	(6)

The resulting entropy values were converted from J·K-1 to J·mol-1·K-1. Although SSchl represents an upper-bound estimate, it provides a robust basis for comparing ΔS among different samples when the same analysis workflow is applied consistently.

(4) Quasi-Harmonic Conformational Entropy

For the quasi-harmonic approximation, the eigenvalues λiwere used to define the effective angular frequencies of the principal modes:

ωi=kBTλi,νi=ωi2π	(7)

Each principal fluctuation mode was then treated as a quantum harmonic oscillator. The entropy contribution of mode iwas calculated as

Si=kBxiexp⁡(xi)-1-ln⁡1-exp⁡(-xi),xi=hνikBT	(8)

The total quasi-harmonic conformational entropy was obtained by summing over all modes:

SQH=iSi	(9)

The final entropy values were likewise reported in J·mol-1·K-1